Machine Specifications

Instrument: Rigaku Ultima IV, University of Alberta, Department of Earth and Atmospheric Sciences

Radiation Source: Cobalt tube at 38 kV and 38 mA

| Anode | Wavelength (Å) |  |  |
| --- | --- | --- | --- |
|  | Kα1 (100) | Kα2 (50) | Kβ1 |
| Co | 1.78900 | 1.79283 | 1.62083 |

Focusing Geometry: Bragg Brentano Mode

Detector: D/Tex Ultra with Fe Filter (K-beta filter)

Slit sizes used are:

Divergence Slit - 2/3deg

Divergence Height Limiting Slit - 10mm

Scattering slit - open

Receiving Slit - open

Scan Information:

Range: 5 to 80°

Scan Axis: 2Θ/Θ

Scan Mode: Continuous

Sampling Width (Step Size): 0.0200°

Scan Speed: 1.20 deg/min

Spin: 15 rpm

Data was converted using JADE MDI 9.6 software. Phase identification was done using DIFFRAC.EVA V5 software using the 2022/2023 ICDD PDF 4+ and PDF 4+/Organics databases.

Sample Prep:
Samples were prepared as front loaded well mounts.