Iodine Adsorption on Silver-Exchanged Titania-Derived Adsorbents

# Lan Wua, James A. Sawadaa, Daniel B. Kuznickib, Tetyana Kuznickia,

# Steven M. Kuznickia*

a: Department of Chemical and Materials Engineering, University of Alberta, Edmonton, Alberta, Canada T6G 2V4

b: Maxxam Analytics, 9331 48 St NW, Edmonton, Alberta, Canada T6B 2R4

*Corresponding author.  Tel: 1.780.492.8819, Fax: 1.780.492.8958 E-mail address: steve.kuznicki@ualberta.ca

Abstract:

I-129 is a hazardous fission product due to its long half life and ability to bioaccumulate. Silver mordenite has been studied for the removal of I-129 because of its hydrothermal stability arising from a high Si/Al ratio which subsequently limits its silver loading and iodine capacity. Titanosilicate ETS-10 and the sodium nanotitanate ETS-2 were exchanged to over 35 wt% silver and exposed to saturated iodine vapour at 80 °C under dry and humid conditions.  The results indicate that the silver on these materials is reactive toward iodine and that the majority of the silver ions are utilized.

Keywords:   iodine removal, Ag-exchanged adsorbent, titanosilicate ETS-10, nanotitanate ETS-2

1. Introduction

Radioactive iodine I-129 is a common product of nuclear fission and is of particular concern due to its exceptionally long half-life and, when released, its ability to integrate into the environment. I-129 can be released as an off-gas during fuel dissolution or during a catastrophic upset in the reactor condition.  The vented gas in either case will likely contain both organic (methyl iodide) and inorganic (I2) radionuclides in a background of high temperature steam and radiolytic oxygen.

Wet processes have been established that remove iodine by contacting the gas stream containing iodine with an aqueous solution of chemicals that are chemically reactive toward iodine. Liquid contactors can contain 20M nitric acid (Iodex Process) [1] or a mixture of mercury and concentrated nitric acid (Mercurex Process).  Liquid processes are attractive because they are scalable and the chemical specificity of the reaction is high. However, these processes have a stronger preference for inorganic iodine compared to organic iodine and the requirements and materials for handling and recycling such corrosive and toxic chemicals are demanding and costly

To overcome the limitations of liquid contactors, packed bed adsorbers are used that incorporate a dry, pelletized or granular adsorbent. The solid adsorbent is thus required to have a chemical affinity for iodine to selectively remove iodine from the gas stream.  By far one of the most widely used methods of radioiodide abatement is the use of activated carbon.  Activated carbon forms the backbone of most emergency filtered air discharge systems as part of all nuclear power plants. The carbon is impregnated with, urotropine (hexamethylene tetramine), (1, 4-diazobicyclo (2, 2, 2) octane) or most commonly triethylenediamine (TEDA) [3]. The filtration system may be worked into any plant where either reprocessing or venting must take place which can force the vented I-129 in both elemental and organic form through the carbon bed allowing sorption to take place at relatively high levels [4].

This system however, is not without flaws. First, the age of the carbon has a noticeable impact on the effectiveness of the sorption of the carbon bed [5]. Moisture too, poses a problem, as the absorption of any water by the carbon bed will result in a decrease in sorption efficiency [5]. Nitrogen oxides, often present in the off streams created by fuel reprocessing, will poison the carbon bed resulting again in efficiency drop [6]. Finally the carbon sees a decreasing retention rate with an increase in temperature compounded by the low ignition point of the carbon itself [6].

An alternative to natural-source activated carbon is organic ion-exchange resins.  Amberlyst A-27 showed effective iodine sequestration but lacked selectivity as the associated Te-123 was co-adorbed [7]. Anion-exchange resins based on polyethylenimine-epichorlohydrin were studied as an alternative to activated carbon zeolite molecular sieves. The resins displayed significant capacity for iodine though their capacity fell off rapidly with the introduction of competing anions in solution [8]. As with any organic material, the thermal stability of such resins is limited and so inorganic supports are preferred to allow the adsorbent to operate under a wider range of conditions.

To meet the challenges associated with selectively adsorbing iodine enhanced selectivity toward iodine is needed. Metallic silver granules have been used to pre-concentrate iodine from a background of Zn-65, Co-60, and Te-123m. The iodine was removed quantitatively over the course of several hours while all other competing species remained in solution [9]. Ionic silver is likewise a thermodynamically favourable species due to its capability to remove both inorganic and organic forms of iodine at elevated temperatures and in the presence of steam.  Silver-exchanged organic resins packed into columns have even been shown to be effective at removing radioiodine from highly acidic, aqueous streams [10]. Silver nitrate coated ceramic saddles [11] work effectively as they present a large surface area to the gas stream and the support has ample thermal and chemical stability to survive the adsorption environment. The silver nitrate, however, is prone to being stripped from the support when water vapour condenses on the surface and dissolves the silver nitrate film. The same obstacles apply to any inorganic material impregnated with a soluble silver salt.

Ion exchange onto porous inorganic supports is a recognized method to “fix” the silver onto the surface of the support.  Mordenite is a specific type of natural aluminosilicate zeolite and is of particular interest in the removal of radioiodine from off gas streams. Under experimental conditions a loading capacity of 34 mg methyl iodide per gram of substrate was measured, with the capacity for elemental iodine being about five times higher [12]. It has been shown that the loading capacity of silver impregnated mordenite peaks at 5% weight of silver, with capacity leveling off at increased levels of silver [13].  Furthermore, it has been shown to be highly resistant to NOx poisoning [13]. The chemical stability of silver-exchanged mordenite comes at the cost of its cation-exchange capacity. Assuming the performance threshold could be moved, mordenite will have a maximum silver loading on the order of 15 wt% which limits the theoretical maximum amount of iodine it can adsorb to approximately 0.2 g I/g Ag-MOR. A fundamental challenge to all molecular sieves arises from the very high levels of humidity present in these streams. In the event of condensation, the adsorbent will be inactivated due to the condensation of water in the hydrophilic pore system.

Titania-derived adsorbents are a novel solution to the iodine adsorption challenge. ETS-10 is a titanosilicate molecular sieve composed of linear, octahedral chains of titania isolated from each other by channels composed entirely of silica. This unique composition lends ETS-10 a chemical stability which enables it to resist acid conditions that would progressively damage all but the most dealuminated zeolites [14]. The silica pore walls of ETS-10 are intrinsically hydrophobic which gives the molecular sieve a unique water adsorption profile. At temperatures near ambient the material has a relatively rectangular adsorption profile while at temperatures above 60 °C this profile rapidly collapses [15]. The water capacity of ETS-10 decreases by almost an order of magnitude between 25 and 100 °C at a partial pressure of 0.02 bar compared to zeolite 4A whose capacity decreases by only 30% under the same conditions [16].

The water adsorption characteristics for molecular sieves is driven predominately by the molecular sieves’ framework and less so by the ions resident in the framework. The adsorption characteristics for Ag-ETS-10 are expected to be comparable to that for the published material though the standardized water capacity (wt %) will change significantly due to the contributing weight of the silver in the framework. The unique adsorption characteristics of ETS-10 should protect the Ag-ETS-10 adsorbent from flooding under high humidity at elevated temperature.

ETS-2 is a high surface area sodium titanate synthesized via alkaline digestion of nanoparticles of TiO2. The caustic treatment converts the surface of the particles to negatively charged TiO3- groups which are offset by exchangeable, charge-balancing cations. ETS-2 has no measurable microporosity and its surface area is entirely the result of the external surface area of the platelets, which can exceed 300 m2/g. Pairing the ion exchange properties of a zeolite with a non-porous support limits the risk of water condensing in the pore structure, which can foul the adsorbent and reduce its ability to remove iodine from a vent stream.

Ag-ETS-2 [17] and Ag-ETS-10 [18] are known to form metal nanodots on their surfaces. Ag-ETS-10 had been shown to be highly selective toward the adsorption of noble gases from air [18, 19] and the strength of the interaction suggests that the silver is a particularly active form. The state of the silver on these two materials, however, is not precisely known and may consist of metallic, ionic, or charged-metal clusters or combinations of these. As a result it could not be predicted how reactive the silver on the surface of these two materials would be toward iodine adsorption.

Testing was undertaken to understand the adsorption limit of these titanate-derived adsorbents under both dry and fully humid conditions. The testing was not constructed to mimic a vent stream from a reactor or a fuel digestion process but to determine whether some or all of the silver on the surface of the adsorbents was active and accessible for inorganic iodine adsorption. Also of interest was the influence of moisture on the adsorption capacity of the silver-impregnated materials and whether a high level of humidity would negatively affect the iodine capacity for either adsorbent.

2. Experimental

2.1 Synthesis of Substrate Materials

In this work, the substrate material of titanosilicate molecular sieves, Na-ETS-10, was synthesized by the method described elsewhere [20]. Na-ETS-2 was hydrothermally synthesized by the method developed by Shi et al. [17].

2.2 Silver Ion-Exchange

The as-synthesized Na-ETS-10 and Na-ETS-2 were silver-exchanged by exposing the quantities of powder to a silver nitrate solution using a weight ratio of 1 part solid to 2 parts silver nitrate (99+% AgNO3, Fisher) in 10 parts of de-ionized water. The silver nitrate was first dissolved in the water before the powder was added. The mixture was slurried in a tightly capped plastic bottle before being placed in a convection oven. The samples were held static at 80 °C for 24 h. The resultant materials were filtered and washed with de-ionized water, dried at 80 °C, and then annealed at 150 °C for 4 h in air. The ion-exchanged samples are referred to as Ag-ETS-10 and Ag-ETS-2.

2.3 Iodine Adsorption

Both the as-synthesized and silver-exchanged samples were exposed simultaneously in a common vessel. A quantity of powder was spread thinly across the bottom of the jar and a corresponding quantity of iodine crystals contained in a 5 mL glass crucible was placed inside the jar before the lid was screwed on tightly. For experiments using moisture, the requisite amount of water was weighed into an open 10 mL glass vial and placed inside the jar to humidify the contents of the jar.

Adsorbents were exposed to dry iodine in a sealed container at 80 °C for 72 h with the weight ratio of 1 part sample to 1 part elemental iodine. Humidity was introduced by adding 5 parts deionized water to the container.  The samples were thus exposed to a partial pressure of water of approximately 0.47 bar and 0.024 bar partial pressure I2 [21].

Once exposed to I2, the samples were heated to sublimate off excess I2 that may have condensed on the surface. All silver-exchanged samples were heated at 250 °C in a tube furnace under a constant flow of air for 24 hours to ensure any excess iodine was sublimated and removed from the surface of the adsorbents. The iodine-exposed, as-synthesized materials were sublimated in air at 100 °C in a forced convection oven for 24 hours.  The silver samples were subjected to a higher sublimation temperature (roughly half the melting point of AgI) to ensure that any physisorbed iodine was completely removed from the surface such that any iodine measured on these samples should be associated with AgI. All of the composition data reported for the iodine-exposed samples are for the samples heat-treated under their respective conditions.

2.4 Characterization

The phase purity of the materials was determined by X-ray diffraction (XRD) using a Rigaku Geigerflex 2173 equipped with a Co tube and a vertical goniometer having a graphite monochromator. The surface morphology and elemental composition of the as-synthesized, silver-exchanged, and I2 exposed samples were examined by using a JEOL 6301F field emission scanning electron microscope and a Zeiss EVO MA 15 equipped with a Bruker Silicon Drift Detector for Energy Dispersive X-Ray analysis.

3. Results and Discussion

3.1 Characterizations of Adsorbents

The powder XRD patterns (Figure 1) confirms the structure and purity of both adsorbents. ETS-10 has a typical powder diffraction pattern resulting from the micron-scale crystallites [20] while the pattern for semi-crystalline ETS-2 shows several small, broad peaks above a relatively flat baseline characteristic of the scale of the nano-platelets [17].

Figure 1. XRD pattern of as-synthesized titania-derived adsorbents

The BET surface area analysis indicates that Na-ETS-10 has a surface area of 350 m2/g while the Na-ETS-2 has a BET surface area of 260 m2/g. The t-plot for the isotherm confirms the absence of any measurable amount of micropores for ETS-2.

The chemical composition of the as-synthesized materials determined by energy dispersive X-ray analysis is shown on Table 1.  The composition for Na-ETS-10 is typical for this adsorbent where some potassium is needed to template the structure. The small amount of silicon present in the ETS-2 sample is due to the addition of silica as a buffer in the titanate synthesis mixture. The silica in the sample is present as a separate, precipitated phase and is not incorporated into the sodium nanotitanate.

Table 1. EDX data for as-synthesized adsorbents

|  | Atomic % |  |  |  |
| --- | --- | --- | --- | --- |
|  | Na | K | Ti | Si |
| ETS-10 | 10.94 | 1.84 | 4.86 | 22.18 |
| ETS-2 | 7.52 | 0 | 19.81 | 2.69 |

Silver content loaded by Ag-ion exchange on Ag-ETS-10 is equal to 35 wt% and on Ag-ETS-2 – 39 wt%. Both adsorbents display a high gravimetric silver loading. The silver loading on ETS-10 is calculated to be 35 wt% while on ETS-2 it approaches 40 wt%.

3.2 Iodine Adsorption

Both the as-synthesized and silver-exchanged materials were tested for iodine adsorption under both dry and wet conditions. The as-synthesized samples displayed some capacity for I2 which was anticipated due to the excess iodine used (Table 2). The observation that some I2 remains on the solid after sublimation suggests that the surface of the adsorbents have some stabilizing influence on iodine that lowers its vapour pressure. The data in Table 2 shows that the presence of moisture suppresses the amount of iodine adsorbed on the samples by a factor of about three. This interference effect is consistent with a competitive adsorption model where the water molecules will occupy the majority of the most energetic adsorption sites and thus leave fewer sites available for I2 to adsorb.

Table 2. Iodine loading and atomic ratio of I/Ag for adsorbents exposed to 0.024 bar I2 and 0.47 bar H2O in air

|  | Exposure | Iodine (wt%) | I/Ag |
| --- | --- | --- | --- |
| Na-ETS-10 | Dry | 3.3 | - |
|  | Wet | 1.1 | - |
| Na-ETS-2 | Dry | 3 | - |
|  | Wet | 1.3 | - |
| Ag-ETS-10 | Dry | 22.2 | 0.87 |
|  | Wet | 17.1 | 0.54 |
| Ag-ETS-2 | Dry | 9.6 | 0.75 |
|  | Wet | 9.4 | 0.68 |

All four iodine-exposed, silver-exchanged samples (post-sublimation) were coloured a bright lemon yellow; a colour characteristic of silver iodide. By contrast, the iodine exposed as-synthesized samples were indistinguishable from their parent materials.

The mechanism for the reaction between the solid and the I2 vapour is unknown exactly and depends somewhat on the state of the silver in the adsorbents. The silver is introduced onto the sieves via an ion exchange process which ensures that the metal is in the ionic form. Whether the state of silver changes during the (post-exchange) drying step or whether exposure to iodine vapour alters the metals’ state has not been established. Assuming that the silver remains ionic then the state of the reaction pathway may mirror that established for AgNO3.

Using silver nitrate as a model for an ionic salt, the redox chemistry follows a path where the framework is reduced [22]. The equations have been adapted from the source to reflect that titanate (TiO3-) can be considered the elementary counterbalancing anion for ETS-2 and ETS-10.

6AgTiO3 + 3I2 4AgI + 2AgIO3 + 6TiO2                                                                    (Equation 1)

The I/Ag ratio for the reacted samples defines the silver utilization and provides insight into the amount of silver in the adsorbents that is reactive toward inorganic iodine. The stoichiometry in Eq. (1) indicates a I/Ag ratio of unity for all silver iodide complexes and so values less than unity for this ratio indicate incomplete utilization of the silver while values larger than unity suggest some elemental iodine remains on the surface of the solids.

The I2 adsorption results for the silver exchanged samples are provided in Table 2. Unlike the as-synthesized adsorbents, these samples retain a significant mass of iodine after sublimation. The iodine loadings for both the wet- and dry-exposed ETS-2 samples are roughly equivalent while for ETS-10 there is a reduction in capacity for the sample exposed to wet iodine. The I/Ag ratio calculated for these samples suggests that, under dry conditions, the majority of silver is accessible and reactive toward inorganic iodine.  The trend in the I/Ag ratio suggests that the presence of moisture has a more significant effect on ETS-10 compared to ETS-2 because the I/Ag ratio falls, respectively, by 40% and 10% compared to their dry utilizations. This contrast suggests a mechanism where the nano-pore structure in ETS-10 concentrates the water vapour which impedes iodine access to the reactive silver sites.  ETS-2, being completely non-porous, does not display this sensitivity.

The SEM micrographs for ETS-2 showed no discernable change in the nano-platelet morphology pre- and post-exposure under both dry and wet I2. The Ag-ETS-10 samples, however, did show a remarkable difference depending on whether the I2 exposure was carried out under wet or dry conditions. Figure 2a is a characteristic SEM micrograph for the Ag-ETS-10 adsorbent exposed to dry I2 vapour. The knobs on the surface of the crystallites do not appear in the as-synthesized material nor do they manifest in the crystallites for Ag-ETS-10 exposed to wet I2 vapour (Figure 2b).  The small particulates distributed across the surface of the sample exposed to wet I2 are normally observed on silver-exchanged samples of Ag-ETS-10 and have a composition indistinguishable from the large crystallites.

(a)

(b)

Figure 2.  SEM micrographs for (a) Ag-ETS-10 exposed to dry I2 vapour and (b) Ag-ETS-10 exposed to wet I2 vapour.

The composition of the knobs was compared against that of the crystal face through EDX by focusing the beam on the different components of the sample. The results of the analysis are provided in Table 3 and show that the knobs are composed virtually entirely of AgI. The surface of the crystallite shows the elements characteristic of ETS-10 and includes a ratio of AgI that suggests a portion of the reacted silver remains inside the framework.

Table 3.  Composition of crystal and knobs by EDX

|  | Norm. wt.% |  |  |  |  |  |  | Mole ratio |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | I | Ag | Na | K | Ti | Si | O | I/Ag |
| Crystal | 5.16 | 6.18 | 0.13 | 1.97 | 18.93 | 36.10 | 31.35 | 0.71 |
| Aggregate | 48.40 | 48.50 | 0.10 | 0.30 | 0.08 | 0.92 | 1.74 | 0.85 |

The cause of the formation of the AgI knobs is uncertain. Solid-state mobility of AgI from the core of the ETS-10 crystals to the surface is unlikely to take place during reaction since the reaction takes place at a temperature (80 °C) far below even half of the melting point of AgI. There is a possibility that the knobs are formed during the sublimation step but, in this case, one would expect to see them on all samples. It has been established that, under the right conditions, silver ions can migrate to the surface of a molecular sieve and form knobs on the surface [23]. Generally this process is promoted under reducing conditions where the silver is replaced by hydrogen ions. The formation of the AgI knobs could be the result of a progressive migration of silver from the interior of the crystals to the surface where they can react to form the AgI knobs.

The absence of silver iodide knobs on the surface of the Ag-ETS-10 crystals that had been exposed to wet I2 vapour, could be due to a suppressing effect that the water exerts on silver migration through the sieve, although the mechanism for such an influence has not yet been established. Alternatively, there may be a critical level of silver required to grow the knobs on the surface of the crystallites so the sample exposed to humid I2 may not have reached the point where such knobs can form and that’s why its lower utilization. Any practical application of iodine removal will involve high levels of humidity, therefore maximizing silver utilization under humid conditions remains a priority. To this end, Ag-ETS-2 is a superior adsorbent as it displays the least sensitivity toward moisture yet maintains the chemical and hydrothermal stability of its titanosilicate cousin.

Conclusions

These results confirm that the silver present in both ETS-2 and ETS-10 is in a state reactive toward inorganic iodine. With silver loadings greater than 35 wt% these materials significantly exceed the silver capacity for siliceous aluminosilicate molecular sieves without sacrificing the hydrothermal stability of such porous frameworks. Gravimetric iodine loadings between 9 and 22 wt% were measured depending on the adsorbent and the exposure conditions. The formation of significant amounts of AgI was confirmed by both optical and SEM/EDX measurements. The high surface area, non-porous Ag-ETS-2 adsorbent had a silver utilization of about 70% and demonstrated only a minor sensitivity toward moisture. The combination of high silver loading, framework thermal and hydrothermal stability, and insensitivity toward moisture makes Ag-ETS-2 a particularly promising candidate for radioiodine removal from nuclear process streams.

References:

[1] Burger LL, Burns RE (1979) Technical requirements for the control of 129I in a nuclear fuels reprocessing plant. http://www.osti.gov/scitech/biblio/5840650. Accessed 17 March 2014

[2] Kubota T, Fukutani S, Ohta T, Mahara Y (2013) Removal of radioactive cesium, strontium, and iodine from natural waters using bentonite, zeolite, and activated carbon. J Radioanal Nucl Chem 296:981–984

[3] Ampelogova N, Kritskii V, Krupennikova N, Skvortsov A (2002) Carbon-fiber adsorbent materials for removing radioactive iodine from gases. Atomic Energy 92:336-340

[4] Wren JC, Moore CJ, Rasmussen MT, Weaver KR (1999) Methyl iodide trapping efficiency of aged charcoal samples from Bruce-A emergency filtered air discharge systems. Am Nucl Soc 125:28-39

[5] Kepak F (1990) Removal of gaseous fission products by adsoption. J Radioanal Nucl Chem 142:215–230

[6] Rastunov LN, Magomedbekov EP, Obruchikov AV, Lomazova LA (2011) Evaluation of the sorbet layer thickness in iodine filters. Atomic Energy 110: 68-72

[7] Kandil SA, Farag SA, Khalifa KF, Saleh ZA (2012) An improvement of radioiodine separation from tellurium oxide target through the bed depth of ion-exchanger J Radioanal Nucl Chem 293:75–79

[8] Sarri S, Misaelides P, Noli F, Papadopoulou L, Zamboulis D (2013) Removal of iodide from aqueous solutions by polyethylenimineepichlorohydrin resins. J Radioanal Nucl Chem 298:399–403

[9] Mostafa M, El-gharbawy AF, El-Absy MA, Soliman SE, Aly FA (2014) Preconcentration of radioiodine as AgI and purification from radiotellurium waste. J Radioanal Nucl Chem DOI 10.1007/s10967-014-2988-2

[10] Decamp C, Happel S (2013) Utilization of a mixed-bed column for the removal of iodine from radioactive process waste solutions. J Radioanal Nucl Chem 298:763–767

[11] Soelberg NR, Garn TG, Greenhalgh MR, Law JD,1 Jubin R, Strachan DM, Thallapally PK (2013) Radioactive iodine and krypton control for nuclear fuel reprocessing facilities. Sci Technol Nucl Install, Article ID 702496, 12 pages

[12] Jubin RT (1980) Organics iodine removal from simulated dissolver off-gas streams using silver-exchanged mordenite. Presentation at the 16th DOE Nuclear Air Cleaning Conference, San Diego, California, October 20-23

[13] Jubin RT (1982) Organics iodine removal from simulated dissolver off-gas streams using partially exchanged silver mordenite. Presentation at the 17th DOE Nuclear Air Cleaning Conference, Denver, Colorado, August 2-5

[14] Kuznicki SM, Anson A, Segin T, Lin CCH (2011) Modified ETS-10 zeolites for olefin separation. US patent 8,017,825

[15] Kuznicki SM, Garfinkel HM, Thrush KA (1993) Use of crystalline molecular sieves containing charged octahedral sites in cyclic desiccating processes. World patent 9,300,152

[16] Tanchuk B, Sawada JA, Rezaei S, Kuznicki SM (2013) Adsorptive drying of CO2 using low grade heat and humid, ambient air. Sep Purif Technol 120: 354–361

[17] Shi M, Lin CCH, Wu L, Holt CMB, Mitlin D, Kuznicki SM (2010) Nanosilver particle formation on a high surface area titanate. J Nanosci Nanotechnol 10: 8448-8451

[18] Kuznicki SM (2012) Titanosilicate molecular sieve supported metallic nanodots, and methods of use to adsorb noble gases. US patent 2012/0144999 A1

[19] Anson A, Kuznicki SM, Haastrup T, Wang Y, Kuznicki T, Sawada JA, Eyring EM, Hunter D (2008) Adsorption of argon, oxygen, and nitrogen on silver exchanged ETS-10 molecular sieve. Microporous and Mesoporous Mater 109: 577-580

[20] Kuznicki SM (1991) Large-pored crystalline titanium molecular sieve zeolites. US Patent 5,011,591

[21] Honig RE, Kramer DA (1969) Vapor Pressure Data for the Solid and Liquid Elements. RCA Review 30

[22] Patil KC, Rao CNR (1967) The silver nitrate-iodine reaction: Iodine nitrate as the `

[23] Sun T, Seff K (1994) Silver clusters and chemistry in zeolites. Chem Rev 94: 857-870